2.0μm emission investigated in Ho3+/Yb3+ codoped germanate-tellurite glasses

Yapei Peng,1, 2 Junjie Zhang,3and Long Zhang1 *

1Key Laboratory of Materials for High Power Lasers, Shanghai Institute of Optics and Fine Mechanics, Chinese Academy of Sciences, Shanghai 201800, China

2University of Chinese Academy of Sciences, Beijing 100039, China

3China Jiliang University, Hangzhou 310018, China

ABSTRACT

2.0μm emission property of a new germanate-tellurite glass with Ho3+/Yb3+ codoping is synthesized and analyzed. Efficient 2.0μm emission of Ho3+ ions sensitized by Yb3+ ions from the host glass was observed under 980nm pumping. Based on the measured absorption spectra, the Judd-Ofelt parameters were calculated and discussed. Strong emission around 2.0μm is observed and the sensitization of Ho3+ is realized by codoping of Yb3+ ions. The radiative transition probability and radiative lifetime of Ho3+:5I7→5I8 in GTLaF-1 are 88.22s-1 and 11.33ms, respectively. The maximum emission cross section of Ho3+:5I8→5I7 transition is 4.36×10-21 cm2 around 2.0μm. The energy transfer efficiency and energy transfer rate are calculated to be 81.2% and 6506.55s-1 in GT glass. The energy transfer efficiency is calculated and fitted the decay signals. The good spectroscopic properties suggest that Ho3+/Yb3+ codoped germanate-tellurite glass may become an attractive host for developing solid state lasers operating in the mid-infrared.

Keyword: Rare-earth ions, germanate-tellurite glass, 2m laser

Fig. 1 Absorption and emission cross section of Ho3+:5I8→5I7 in GTLaF-1 glass.

* Corresponding author: lzhang@siom.ac.cn